
GENERAL NOTES FOR STREET IMPROVEMENT PLANS
1. CONTRACTOR SHALL BE RESPONSIBLE FOR CLEARING OF THE PROPOSED WORK AREA AND RELOCATION COSTS OF ALL EXISTING UTILITIES.  ALL UNDERGROUND FACILITIES WITH LATERALS SHALL BE IN PLACE PRIOR TO PAVING THE STREET SECTION, INCLUDING, BUT NOT LIMITED TO SEWER, WATER, ELECTRIC, GAS, DRAINAGE, TELEPHONE, CABLE TV, ETC.
2. THE CONTRACTOR SHALL TAKE ALL NECESSARY PRECAUTIONS TO PROTECT ADJACENT PROPERTY OWNERS FROM ANY AND ALL DAMAGE THAT MAY OCCUR FROM STORM WATER RUNOFF AND/OR DEPOSITION OF DEBRIS FROM ANY AND ALL WORK IN CONJUNCTION WITH CONSTRUCTION OF THESE IMPROVEMENTS.

3. THE CONTRACTOR SHAL BE RESPONSIBLE FOR ALL DAMAGES TO ON-SITE, OFF-SITE, AND ADJACENT UTILITIES, FACILITIES, AND PROPERTY AND SHALL CARRY SUFFICIENT INSURANCE TO PROTECT THE CITY AND THE ADJACENT PROPERTY.
4. DEPTH OF BASE MATERIALS AND A.C. PAVING SHALL BE DETERMINED BY THE R-VALUE METHOD, DESIGNATED AS TEST NO. 301-F OF THE STATE OF CALIFORNIA DEPARTMENT OF TRANSPORTATION, HIGHWAY DESIGN MANUAL.
5. STREET PAVING SHALL BE INSTALLED IN TWO (2) LIFTS: TOP COURSE 1” THICK (MINIMUM) 1/2” A.C. PG-70-10 (D1) AND BOTTOM COURSE 2” THICK (MINIMUM), 3/4” A.C. PG-70-10 (C2).
6. WHEEL CHAIR RAMPS SHALL BE CONSTRUCTED AT ALL CURB RETURNS IN CONFORMANCE WITH CITY STANDARD DRAWING S-26 AND ADA REQUIREMENTS.
7. THE CONTRACTOR SHALL INSTALL STREET NAME AND STOP SIGNS CONFORMING TO THE CITY STANDARD DRAWING S-27. 

8. ALL MANHOLE COVERS AND WATER VALVE COVERS SHALL BE ADJUSTED TO GRADE AFTER THE STREETS HAVE BEEN FINAL PAVED PER CITY STDS.
9. ALL PRIVATE STREETS AND DRIVEWAYS SHALL BE CONSTRUCTED TO THE STRUCTURAL SECTION DETERMINED BY THE CITY ENGINEER.
10. TRIM (SAWCUT) EDGE OF EXISTING PAVEMENT WHERE NEW PAVING JOINS EXISTING TO FORM A CLEAN, SMOOTH STRAIGHT LINE.
11. THE CONTRACTOR SHALL NOTIFY THE CITY OF COACHELLA ENGINEERING DEPARTMENT, 619-398-5744, 72 HOURS PRIOR TO STARTING ANY STREET WORK.
12. ALL WORKS SHALL CONFORM WITH THE CITY OF COACHELLA IMPROVEMENT STANDARDS AND SPECIFICATIONS AND THE STANDARD SPECIFICATIONS FOR PUBLIC WORKS CONSTRUCTION (GREEN BOOK) LATEST EDITION AND THESE PLANS.

13. This was a duplicate of #2
14. THE CONTRACTOR SHALL BE RESPONSIBLE FOR ALL WORK AND SHALL MAINTAIN ALL FACILITIES COMPLETE AND INCOMPLETE UNTIL ACCEPTED BY THE CITY.
CITY OF COACHELLA

STREET NOTES

CITY OF COACHELLA

STREET NOTES




